COLLECTION OF IECEx / ExTAG DECISIONS

| Standard: IEC 60079-0:2011 | Clause: 7.1.2.2 | Date: 2014 05 13 Originator of proposal: SP Technical Research Institute of Sweden |
| --- | --- | --- |
| Subject: Specification of RTI Status of document: Approved | Key words: Specification of plastic material in enclosure |  |
| Question: Is it acceptable to use the most favourable value of “RTI –mechanical impact” and “RTI – mechanical strength”, for a plastic material in the enclosure? For example, if a material has specified RTI –mechanical impact = 105 °C and RTI – mechanical strength = 120 °C, could the value 120 °C then be used to satisfy the requirement in the standard? Answer: Yes (as IEC 60079-0:2011 specify not more than “RTI-mechanical”). Background: According to section 7.1.2.2 d) specification of “RTI – mechanical” is acceptable for plastic materials in enclosures. In earlier editions of the standard specification of “RTI mechanical impact” was required. |