COLLECTION OF IECEx / ExTAG DECISIONS

| Standard: ISO/IEC 80079-34 | Clauses: A.3.2 |  |
| --- | --- | --- |
| Subject: Verification Requirements for Flameproof Castings Status of document: Approved | Key words: Flameproof enclosures Verification Castings 100% visual inspection | Date: Originator of proposal: UL TC/SC involved: IEC/TC 31 and IEC/SC 31M |
| Question: Does A.3.2 require 100% visual inspection of castings to verify wall thickness, flaws, inclusions, blow holes and porosity? Answer: No. Annex A is Informative, not Normative. Therefore, it merely provides guidance regarding issues to consider. Therefore, when addressing Product realization, such as under 7.1 and 7.5.1, control of the casting process is needed regarding wall thickness, flaws, inclusions, blow holes and porosity. This control can be accomplished by 100% visual inspection, or by another means deemed appropriate based on the ability of the manufacturer to effectively control production. |